## Slide 1
RF SQUID Metamaterials For Fast Tuning
Daimeng Zhang, Melissa Trepanier, Oleg Mukhanov, Steven M. Anlage
NSF-GOALI ECCS-1158644
Fall 2013 MRS Meeting
2 December, 2013
Phys. Rev. X (in press); arXiv:1308.1410
Notes: 15 Minutes including questions

## Slide 2
Outline
Brief Introduction to Superconducting Metamaterials and SQUIDs
Design of our RF SQUIDs
Results (Tunability with Temperature, DC Flux, RF Flux)
Single RF SQUID
RF SQUID Array
Modeling and Comparison with Data
Tuning Speed
Future Work and Conclusions

## Slide 3
Why Superconducting Metamaterials?
The exciting applications of metamaterials:
Flat-slab Imaging
“Perfect” Imaging
Cloaking Devices
etc. …
SUPERCONDUCTING METAMATERIALS:
Achieve these requirements!
… have strict REQUIREMENTS on the metamaterials:
Ultra-Low Losses
Ability to scale down in size (e.g. l/102) and texture the “atoms”
Fast tunability of the index of refraction n
Pendry (2004)
l
Steven M. Anlage. "The Physics and Applications of Superconducting Metamaterials," J. Opt. 13, 024001 (2011).

## Slide 4
The Three Hallmarks of Superconductivity
Zero Resistance
I
V
DC Resistance
Temperature
Tc
0
Complete Diamagnetism
Magnetic Induction
Temperature
Tc
0
T>Tc
T<Tc
Macroscopic Quantum Effects
Flux F
Flux quantization F = nF0
Josephson Effects
B

## Slide 5
Macroscopic Quantum Effects
Superconductor is described by a single
Macroscopic Quantum Wavefunction
Consequences:
Magnetic flux is quantized in units of F0 = h/2e (= 2.07 x 10-15 Tm2)
R = 0 allows persistent currents
Current I flows to maintain F = n F0 in loop
n = integer, h = Planck’s const., 2e = Cooper pair charge
Flux F
I
superconductor
Example of Flux Quantization
50 mm
One flux quantum in this loop requires a field
of B = F0/Area = 1 mT = 10 mG
Earth’s magnetic field Bearth ~ 500 mG
Superconducting
Ring

## Slide 6
Gauge-invariant phase difference
Macroscopic Quantum Effects
Continued
Josephson Effects (Tunneling of Cooper Pairs)
Circuit representation of a JJ
DC
AC

## Slide 7
Why Quantum
Josephson Metamaterials?
Josephson Inductance is large, tunable and nonlinear
Resistively and Capacitively Shunted Junction
(RCSJ) Model
Notes: Josephson inductance derived: I = Ic sin(delta). Time-derivative: I. = Ic cos(delta) delta. = Ic (2e/h-bar) V cos(delta) Solve for V = LJ I., giving LJ = Phi_0/[ 2 Pi Ic cos(delta) ]

## Slide 8: SQUIDs
Inductance of Junction in rf SQUID Loop
rf SQUID
dc SQUID (NOT used here)
Operates in the voltage-state
Flux-to-Voltage transducer
V(F)
Lgeo
LJJ
R
C
F
n = integer
A Quantum
Split-Ring
Resonator
Notes: An rf SQUID is a superconducting loop interrupted by a single junction
As opposed to a DC SQUID which usually has two junctions and current leads
The net flux through the loop must be an integer number of flux quanta
So a DC field can induce a current in the loop
The current through the loop and associated phase difference will take on the value necessary to fulfill this requirement
On the bottom left I show the total current circulating through an rf SQUID loop as a function applied flux
There are SQUIDs for which this is not a single-valued function
But all of our SQUIDs are non-hysteretic
On the bottom right I show the Josephson inductance as a function of applied flux
It’s tunable over a wide range of values both positive and negative

## Slide 9
Example of our RF SQUID meta-atom
sc loop
Overlap forms capacitor
Via (Nb)
Niobium Layer 2
Niobium Layer 1
Junction
L
LJJ
R
C
Nb/AlOx/Al/Nb
Nb: Tc = 9.2K

## Slide 10: Tunable RF SQUID Resonance
20
10
f0 (GHz)
Lgeo
LJJ
R
C
resistivity and capacitively shunted junction model
F
Tunability of RF SQUID Resonance
Potential Application:
Tunable band-pass filter for digital radio:
Multi-GHz tuning
Sub-ns tuning time scale
JJ switching on ~ ħ/D ~ ps time scale
Notes: An Rf SQUID can be modeled as an RLC circuit
Using the resistively and capacitively shunted junction model
Applying a flux through the loop of the SQUID changes the JJL and has this effect on the resonant frequency

## Slide 11
Experimental Setup
Nb/AlOx/Al/Nb
Josephson
Junction
Frequency
S21 (dB)
Transmission:
S21 = Vout/Vin
Nb: Tc = 9.2K

## Slide 12
Chart: 
RF power = -70 dBm, @6.5K
Comparison to model estimate
Tuning Range: 9.66 ~ 16.64 GHz
ΦDC/Φ0
Frequency (GHz)
Processed data
Single-SQUID Tuning with DC Magnetic Flux
D|S21|
See similar work by P. Jung, et al.,
Appl. Phys. Lett. 102, 062601 (2013)

## Slide 13
Single-SQUID Tuning with DC Magnetic Flux
Comparison to Model
RF power = -80 dBm, @6.5K
Maximum Tuning: 80 THz/Gauss @ 12 GHz, 6.5 K
Total Tunability: 56%

## Slide 14
Modeling RF SQUIDs
L
LJJ
R
C
F
S21 =
k =
Flux
Quantization
in the loop
Solve for d(t), calculate LJJ, I(t), mr(f)
I(t)
arXiv:1308.1410
Ic

## Slide 15
Single-SQUID Power Dependence
Power Sweep at nominal FDC = 0
Comparison to full nonlinear model
Transparency!
Data and model agree that the single-SQUID “disappears” over a range of incident power
~ BRF2

## Slide 16: Nonlinear Model Calculation of RF Power Dependence
experiment
model
Prf (dBm)
Frequency (GHz)
experiment
Transparency!

## Slide 17: 27x27 RF SQUID Array
output rf wave
Brf
Erf
Waveguide
Input rf wave
Network Analyzer
attenuator
RT amplifier
LNA
80 µm
JJ
via
2 Nb layers
Cryogenic
environment
BDC
a)
RF SQUID array
Single RF SQUID
l / a ≈ 200

## Slide 18: 27x27 RF SQUID Array
DC magnetic flux tuned resonance
Coherent!
46% Tunability

## Slide 19
Coherent Tuning of RF SQUID Array
For example, 2 coupled RF SQUIDs:
The coupled SQUIDs oscillate in a synchronized manner,
even when there is a small difference in DC flux (fDC)
The SQUID resonance blue-shifts with increased coupling,
or increasing the number of SQUIDs in the array
k
k
k=0.1
k=0.2
Bapp
Loop 1
Bind
I
Bapp
Loop 2
Bind
I
Bc
Bc
k = M / L

## Slide 20
Speed of RF SQUID Meta-Atom Tunability
Upper limit: Shortest time scale for superconductor switching is ħ/D ~ 1 ps
Circuit Time scales:
L/R ~ 0.5 ps
RC ~ 0.3 ns
Temperature Tuning:
Generally slow, depending on heat capacity and thermal conductivity
Tuning speed ~ 10 ms
see e.g. V. Savinov, et al. PRL 109, 243904 (2012)
RF Flux Tuning:
Pulsed RF measurements show response time < 500 ns
Quasi-static Flux Tuning:
ns-tuning frequently achieved in SQUID-like superconducting qubits
see e.g. Paauw, PRL 102, 090501 (2009); Zhu, APL 97, 102503 (2010)

## Slide 21
Future Work
JJ wire + SQUID metamaterials for n < 0
Calibrate the cryogenic experiment to extract µ, ε of our metamaterials [J. H. Yeh, et al. RSI 84, 034706 (2013)]
Further investigate nonlinear properties of SQUID metamaterials
  Bistability in bRF < 1 RF SQUIDs
  Multistability in bRF > 1 RF SQUIDs
  Intermodulation and parametric amplification in SQUID arrays

## Slide 22
Conclusions
Successful design, fabrication and testing of RF SQUID meta-atoms and metamaterials
Periodic tuning of resonances over 7+ GHz range under DC magnetic field ~ mGauss.
∆f/∆B ~ 80 THz/Gauss (max) @ 12 GHz, 6.5 K
SQUID meta-atom and metamaterial behavior understood from first-principles theory
RF SQUID array tunes coherently with flux → synchronized oscillations
Metamaterials with greater nonlinearity are possible!
Thanks for your attention!
anlage@umd.edu
Phys. Rev. X (in press); arXiv:1308.1410
Steven M. Anlage. "The Physics and Applications of Superconducting Metamaterials," J. Opt. 13, 024001 (2011)
Thanks to A. V. Ustinov, S. Butz, P. Jung @ Karlsruhe Institute of Technology
and M. Radparvar, G. Prokopenko @ Hypres
NSF-GOALI ECCS-1158644